ISSN 1392-3196

Žemdirbystė. Mokslo darbai, t. 93, Nr. 3 (2006), p. 108-118

UDK  633.52

## LINŲ  PLUOŠTO  ATSKYRIMAS  IN  SITU:  3. Pluošto  IŠEIGOS  ir  kokybės  dinamika

##### Zofija JANKAUSKIENĖ, Algimantas ENDRIUKAITIS

Lietuvos žemdirbystės institutas

Upytė, Panevėžio rajonas

El. p. soja@upyte.lzi.lt

###### Santrauka

2002-2004 m. LŽI Upytės bandymų stotyje tirta, kaip kinta nerautų (stačių) klojėjamų linų, kurie buvo nepurkšti, purkšti raundapu (veikl. medž. glifosatas 360 g l-1)       3 l ha-1 ir purkšti defoliantu reglonu super (veikl. medž. dikvatas 150 g l-1) 2 l ha-1 pluošto išeiga bei kokybiniai rodikliai (lankstumas, stiprumas, kokybės numeris).

Linų klojėjimosi eigai įtakos turėjo meteorologinės sąlygos, tad šio proceso trukmė skirtingais metais buvo nevienoda. Ilgėjant klojėjimo trukmei, pluošto išeiga mažėjo. Visais tyrimų metais didžiausia brukto ilgojo pluošto išeiga buvo gauta nupurškus linus raundapu, tačiau skirtumai tarp variantų ne visada būdavo esminiai (ypač tyrimų pradžioje). Klojėjimosi eigoje pluošto kokybės numeris didėjo (gerėjo). Nepurkštų klojėjamų linų pluošto kokybės numeris buvo mažesnis. Dauguma atvejų raundapu bei reglonu super purkštų linų brukto ilgojo pluošto lankstumas buvo didesnis nei nepurkštų klojėjamų linų, tačiau skirtumai ne visada buvo esminiai. Pluošto stiprumas 2002 m. klojėjimosi eigoje turėjo ryškią tendenciją mažėti, 2003 ir 2004 m. pluošto stiprumo duomenys tyrimų metu įvairavo, bet pastebima ta pati tendencija. Nerauti ir nenupurkšti linai pakankamai atsiklojėjo tik 2002 m., o raundapu ir reglonu super purkštus linus galima rekomenduoti klojėti ir nerautus.

Reikšminiai žodžiai: bruktas ilgasis pluoštas, kokybės numeris, lankstumas, klojėjimas, pluošto išeiga, raundapas, reglonas super, stiprumas.

ISSN 1392-3196

Agriculture. Scientific articles, t. 93, Nr. 3 (2006), p. 108-118

UDK  633.52

### FLAX  FIBRE  SEPARATION  IN  SITU:  3. DYNAMICS  OF  fibre quantity  and  quality

Z. Jankauskienė, A. Endriukaitis

Summary

The study of the effects of Roundup 3 l ha-1 (a.i. glyphosate 360 g l-1) and Reglone Super 2 l ha-1 (a.i. dikvat 150 g l-1) application on the dynamics of scutched long fibre quantity and quality parameters (quality number, flexibility and tenacity) during the dew-retting process of stand-retted flax was done at the Upytė Research Station of LIA during 2002-2004.

The weather conditions exerted a great effect on the dew-retting process, and the duration of this process during the experimental years was different. It was very dry and hot at the end of the growing season and after Roundup and Reglone super application in 2002, dew-retting lasted for 13 weeks. In 2003 the weather conditions were suitable for dew-retting for about 3 weeks after Roundup and Reglone super application, but this process was not completed. Later on the weather became cool and dry and dew-retting continued for 10 weeks.  In 2004 the weather during the dew-retting period was wet but cool, therefore dew-retting continued for 9 weeks. The fibre content decreased during the dew-retting process. The highest fibre content was obtained after Roundup application, but the differences were significant mainly at the end of investigation. The quality number of scutched long fibre increased in the course of dew-retting. It was lower for untreated flax. The flexibility of scutched long fibre was higher for treated flax, but the differences not always were significant. The tenacity indices tended to decrease during the dew-retting process. Stand-retting was successful after Roundup or Reglone Super application while untreated stand-retted flax was completely dew-retted only in 2002, therefore Roundup or Reglone Super application can be recommended for flax stand-retting.

Key words: dew-retting, fibre content, flexibility, quality number, Reglone Super, Roundup, scutched long fibre.